[SECTION 09 62 16 – CONCRETE PLANK [AND WOOD PLANK] FLOORING]

[SECTION 09 64 29 – WOOD PLANK FLOORING]

Concreate Concrete Flooring provides the durability of real burnished concrete floors without the challenges of pouring and finishing a slab. Our concrete planks, just ½ inch thick, have tongue and groove edges and install quickly and cleanly with adhesives.

Concreate Wood Flooring has real wood veneer applied to the same concrete base used for our concrete flooring. This eliminates the swelling and shrinking associated with solid wood flooring.

Use Concrete and Wood Together: Concreate’s concrete and wood flooring products can be used together; they have the same thickness, tongue and groove edges, and installation methods.

SPECIFICATION COORDINATION: This document is available in word processing format at our website. Turn on HIDDEN TEXT to view or print specifier notes. Edit to include only requirements pertinent to Project.

DRAWING COORDINATION: Show flooring locations, orientations or patterns, and colors on Drawings or finish schedules. Show details of special conditions.

DESIGN AND TECHNICAL ASSISTANCE: Concreate – www.Concreate.net, info@Concreate.net, +1 855 265 2116 (UTC/GMT -8:00).

GENERAL

SUMMARY

Section Includes:

[Concrete plank flooring.]

[Wood plank flooring.]

Related Sections:

[Underlayment.] [Leveling compound.]

[Concrete Wall Paneling: Concreate wall panels with matching finish.]

[_____________.]

REFERENCE STANDARDS

ANSI A137.1 - American National Standard Specifications for Ceramic Tile

ASTM E303 – 93 – Standard Test Method for Measuring Surface Frictional Properties Using the British Pendulum Tester

US Environmental Protection Agency (EPA) - Determination Of Volatile Matter Content, Water Content, Density, Volume Solids, And Weight Solids Of Surface Coatings

SUBMITTALS

Coordinate submittals with Division 01 requirements.

Submit:

Manufacturer’s product data and installation instructions for flooring, adhesives, repair and cleaning products, and [_______].

Submit sample copy of manufacturer’s warranty.

[Samples for Color Selection: Submit samples of manufacturer’s standard colors.]

Use above if color selection will be made after Contract Documents are issued. Select below if color selection is included in Contract Documents.

[Samples of Verification: Submit sample of specified colors.]

Letter from flooring manufacturer stating acceptability of installer.

Include following if Owner requires extra stock on hand or custom finishes are specified.

Maintenance material submittals

[Extra Stock Materials: Submit [twenty] [_______] pieces of [each type of] flooring.]

[Repair Materials: Submit [100] [_____] ml of each component and color.]

qUALITY ASSURANCE

Mock-up is not required for typical installations. The following can be used, if required, to mock-up a suite of finishes or to establish workmanship requirements.

Mock-Ups:

[Provide [twenty] [_______] pieces of [each type of] wall paneling as a mock-up at location indicated by Architect showing installation methods to be used.

Approved mock-up [may remain as part of completed construction.] [shall be removed after flooring installation is accepted.]

Installer: Certified firm or subcontractor acceptable to paneling manufacturer.

DELIVERY, STORAGE, AND HANDLING

Comply with manufacturer’s instructions.

Scheduling: Do not deliver to site until project is enclosed, wet work is complete, and building temperature and humidity has stabilized to range acceptable to manufacturer.

Acclimatization: Store products in room where they will be installed for not less than 72 hours.

Warranty

35-year warranty is available for private residences. Five-year warranty is available for other projects. See warranty forms for coverage.

Provide manufacturer’s [35-year] [5-year] limited warranty.

PRODUCTS

Flooring

Product:

Provide Concreate Floor by Concreate LLC, www.concreate.net, info@Concreate.net, +1 855 265 2116.

[Substitutions: Not allowed.]

Substitutions: Use above or below. We know of no product that has appearance and performance similar to Concreate Flooring. If you must include substitution provisions, consider the following language.

[Substitution Limitations: Substitution requests shall be submitted in accordance with Division [00] [01] and shall include:

Documentation that manufacturer has five years experience manufacturing flooring equal to specified products.

Documentation of three projects of size and with quality required on Project. Provide photographs of work, project address, and name and contact information for project designer, contractor, and owner.

Sample four full-size planks demonstrating range of color and appearance [of each type specified].

Submit test reports demonstrating compliance with specified manufacturer’s products.

Description:

Plank shall be a composite of two fully bonded layers:

Base Layer: 10 mm (3/8 inch) thick magnesium oxide concrete with recycled fiber reinforcing.

Top Layer: 4 mm (1/8 inch) thick, with finish specified below.

Profile:

14 mm (1/2 inch) total thickness.

Tongue and groove joints.

Micro-beveled edges.

[Planks with concrete and wood finishes shall be compatible in thickness, installation method and maintenance regimen.]

Volatile Organic Compound (VOC) Emissions: Green Leaf certified, VOC free

Toxin Free: Product is formaldehyde and asbestos free

Concrete Finish:

Plank Size: 1200 x 300 mm (47-1/4 x 11-3/4 inches)

Top Layer: Portland cement concrete with recycled fiber reinforcement.

Custom colors are available for large projects. Contact Concreate for information.

Color: [Natural Grey] [Dark Grey] [Mineral White] [To be selected from manufacturer’s standard colors] [Custom].

Variations in color and appearance characteristic of concrete panels and are acceptable.

Slip Resistance: 0.31 average dynamic coefficient of friction (DCOF) when tested wet in accordance with ANSI A137.1.

Wood Veneer Finish:

Plank Size: 1900 x 150 mm (74-3/4 x 5-7/8 inches)

Veneer:

Contact Concreate for information on additional species.

Species: [Smoked White Oak] [________________]. Variations in color and grain of wood are acceptable.

Certification: FSC 100 Percent from well-managed forests.

Accessories

Adhesive:

Product: Concreate Floor Adhesive.

Volatile Organic Compound (VOC) Emissions: 64 g/l in accordance with EPA Method 24.

Repair Products:

Concrete Flooring: Concreate Concrete Floor Repair Powder and Concreate Floor Repair Oil.

Wood Flooring: Wood filler of type compatible with hardwood flooring and Concreate Floor Repair Oil.

Cleaning and Oiling Products: Types recommended by flooring manufacturer and as manufactured by Wood Care Denmark (WOCA), www.woodcareusa.com.

EXECUTION

Preparation

Inspect substrates to which flooring will be installed. Do not begin installation until:

Substrates are within manufacturer’s tolerances for flatness and deflection.

Substrates are firm and cohesive.

Remove finishes, oil, dust, and other materials that can interfere with adhesive bond.

installation

Install in accordance with manufacturer’s written instructions.

Pattern: [Running bond.] [Random, staggered lengths.] [_______________.][As shown on Drawings.]

Repair and protection

Repair minor scratches and chips with repair materials. If damaged work cannot be repaired to satisfaction of Architect, removed damage work and replace with new materials.

Protect against damage

Final Cleaning

Simple cleaning is sufficient for light wear. Use oiling and buffing provides extra protection where heavy traffic is expected.

Immediately prior to Substantial Completion, [clean] [oil and buff] flooring. Follow manufacturer’s written instructions.

END OF SECTION

Concreate is trademarks of Concreate, LLC. © 2015 by Concreate, LLC. Qualified design and construction professionals may copy for preparation of construction specifications or purchase orders. Issued 2016 October 01; contact Concreate for current information.