SECTION 09 78 19

CEMENTITIOUS INTERIOR WALL PANELING

Concreate Concrete Wall Panels provides the aesthetics and durability of real burnished concrete surfaces that may be installed over standard wall construction and without the challenges and weight of a cast-in-place wall. Our concrete panels, just 1/8 inch thick, install quickly and cleanly with adhesives to approved substrates.

Concreate® Wall Panels are thin concrete panels with the attractive mottled look and smooth feel that only real burnished concrete can provide. They are lightweight and durable and can be easily adhered to walls and other vertical interior surfaces.

SPECIFICATION COORDINATION: This document is available in word processing format at our website. Turn on HIDDEN TEXT to view or print specifier notes. Edit to include only requirements pertinent to Project.

DRAWING COORDINATION: Show location of paneling on Drawings or finish schedules. If necessary, indicate pattern and details of corners, abutments to other materials, and special conditions.

DESIGN AND TECHNICAL ASSISTANCE: Concreate – www.Concreate.net, info@Concreate.net, +1 855 265 2116 (UTC/GMT -8:00).

GENERAL

SUMMARY

Section Includes: Interior concrete wall paneling.

[Product Specified in this Section for Installation in Another Section: Panels to be installed as part of:]

[Architectural woodwork.]

[Ceiling suspension system.]

[___________________.]

Edit following as required.

Related Sections:

[Tolerances for construction of substrates.]

[Flooring: Concreate flooring with matching finish.]

[Blocking to support items mounted through paneling.]

[_____________.]

REFERENCE STANDARDS

ASTM E84/ UL 723 – Standard Test Method for Surface Burning Characteristics of Building Materials

SUBMITTALS

Coordinate submittals with Division 01 requirements.

Submit:

Manufacturer’s product data, and installation instructions for panels, adhesives, repair and cleaning products, and [_______].

Submit sample copy of manufacturer’s warranty.

[Samples for Color Selection: Submit samples of manufacturer’s standard colors.]

Use above if color selection will be made at after Contract Documents are issued. Select below if color selection is included in Contract Documents.

[Samples of Verification: Submit sample of specified colors.]

Letter from paneling manufacturer stating acceptability of installer.

Include following if Owner requires extra stock on hand or custom finishes are specified.

Maintenance material submittals

[Extra Stock Materials: Submit [eight] [_______] pieces of [each type of] wall paneling.]

[Repair Materials: Submit [100] [_____] ml of each component and color.]

qUALITY ASSURANCE

Mock-up is not required for typical installations. The following can be used, if required, to mock-up a suite of finishes or to establish workmanship requirements.

Mock-Ups:

[Provide [eight] [_______] pieces of [each type of] wall paneling as a mock-up at location indicated by Architect showing installation methods to be used.

Approved mock-up [may remain as part of completed construction.] [shall be removed after paneling installation is accepted.]

Installer: Certified firm or subcontractor acceptable to paneling manufacturer.

DELIVERY, STORAGE, AND HANDLING

Comply with manufacturer’s instructions.

Scheduling: Do not deliver to site until project is enclosed, wet work is complete, and building temperature and humidity has stabilized to range acceptable to manufacturer.

Acclimatization: Store panels in room where they will be installed for not less than 72 hours.

Warranty

35-year warranty is available for private residences. Five-year warranty is available for other projects. See warranty forms for coverage.

Provide manufacturer’s [35-year] [5-year] limited warranty.

PRODUCTS

Panels

Product:

Provide Concreate Wall Panels by Concreate LLC, www.Concreate.net, info@Concreate.net , +1 855 265 2116.

[Substitutions: Not allowed.]

We know of no product that has appearance and performance similar to Concreate Wall Panels. If you must include substitution provisions, consider the following language.

[Substitution Limitations: Substitution requests shall be submitted in accordance with Division [00] [01] and shall include:

Documentation that manufacturer has five years experience manufacturing concrete panels equal to specified panels.

Documentation of three projects of size and with quality required on Project. Provide photographs of work, project address, and name and contact information for project designer, contractor, and owner.

Sample four full-size panels demonstrating range of color and appearance [of each color specified].

Submit test reports demonstrating compliance with specified manufacturer’s products.

Description:

Size: 1200 x 600 x 4 mm (47-1/4 x 23-5/8 x 1/8 inch).

Composition: Portland cement concrete with recycled fiber reinforcement.

Color: [Natural Grey] [Dark Grey] [Mineral White] [To be selected from manufacturer’s standard colors] [Custom].

Variations in color and appearance characteristic of natural concrete are acceptable.

Volatile Organic Compound (VOC) Emissions: Green Leaf certified, VOC free

Toxin Free: Product is formaldehyde and asbestos free

Accessories

Adhesive: Concreate Wall Panel Adhesive.

Repair Products: Concreate Concrete Floor Repair Powder and Concreate Floor Repair Oil.

Cleaning Products: Types recommended by panel manufacturer and as manufactured by Wood Care Denmark (WOCA), www.woodcareusa.com.

Outside corners or exposed edges of wall paneling can be left exposed or finished with trim. Extruded aluminum or bronze shapes are among your many choices and can be described below. Show locations on Drawings.

Trim: [______________________________.]

An attractive way to protect the bottom of wall paneling from damage and scuff marks is to use a dark colored strip of Concreate Floor. Show locations on Drawings or in finish schedule.

Baseboard:

Product: Concreate Flooring.

Size: 14 mm (1/2-inch) thick x [[_____] inch] [height shown on Drawings].

Color: [Natural Grey] [Dark Grey] [Mineral White] [To be selected from manufacturer’s standard colors].

Outside Corners: Mitered joint and rounded vertical edge.

Top Edge: Provide smooth, [level] [bevel][rounded] surface..

EXECUTION

Preparation

Inspect substrates to which paneling will be installed. Do not begin installation until:

Work to be installed behind paneling is complete and approved.

Substrates are within manufacturer’s tolerances for flatness and alignment.

Substrates are firm and cohesive.

Remove loose paint, oil, dust, and other materials that can interfere with adhesive bond.

installation

Install in accordance with manufacturer’s written instructions.

Pattern: Install panels [[horizontally] [vertically] in [running] [stack] bond.] [as shown on Drawings.]

Repair and protection

Repair minor scratches and chips with repair materials. If damaged work cannot be repaired to satisfaction of Architect, removed damage work and replace with new materials.

Protect against damage

FINAL CLEANING

Clean paneling immediately prior to Substantial Completion following manufacturer’s written instructions.

END OF SECTION

Concreate is trademarks of Concreate, LLC. © 2015 by Concreate, LLC. Qualified design and construction professionals may copy for preparation of construction specifications or purchase orders. Issued 2016 October 01; contact Concreate for current information.